LOSP-PJ4 金屬薄膜四槍型噴銲機

Two pair gun and double side spray machine

特性Characteristic：

LOSP-PJ4 is a 2 pair spray guns system with two independent spray spaces and spray both side at the same time. User doesn’t need spray two layer processing  two times by manual, and it can finish all capacitor spray processing at the same time by serial work flow.

Every spray gun has the independent motor control, and power supply with the atomizing spray and low air pressure (2.8mp) technical using can save the material and reduce the element surface pollution.

技術規格Specification：

| 項目Item | 規格Specification | 備註Note |
| --- | --- | --- |
| 設備尺寸 Dimension | 長D:4200*寬W:2800*高H:1800 mm |  |
| 電源POWER | 直流/DC 600A |  |
| 噴槍 Spray Gun | 4把/pieces（2Pair） | Atomizing and low temperature using acceptance |
| 清掃槍Aux Clean | 4套/Pieces |  |
| 材料Material | 鋅絲/Zinc：ψ1.6mm~ψ2.0mm | ψ2.0mm |
| 素子尺寸 Element Size | 長度Length：30～150mm 直徑Diameter：ψ20～135mm |  |
| 元件框尺寸 Elements Holder | 高x：500mm / 寬y：500mm | 15 Pieces included per machine |
| 噴金層厚度 Layer thickness | 0.4～1.2mm可調 Adjustable |  |
| 槍與框距離 Spray Distance | 140～250mm可調 Adjustable |  |
| 噴金框移動速度 Holder moving speed | 0～10mm/s可調 Adjustable |  |
| 上下槍移動速度 Gun moving speed | 10-250mm/s可調 Adjustable | Moving control: VFD |
| 送線速度 Wire feeding speed | 2～5m/min可調 Adjustable |  |
| 噴槍出氣量 Air Consumption | 0.8～1.5m3/min（可調Adjustable） |  |
| 電流 Current | 0～110A可調 Adjustable |  |
| 電流波動值 Current change | ±5A |  |
| 電壓Voltage（DC） | 20/22/24/v |  |
| 端面累積溫度 Cumulative temperature | ≤90℃ |  |
| 工作環境噪音 Noise | ≤75dB |  |
| 設備產能 Productivity | 圓形Cylinder（直徑Dia 30mm） 約不小於3000 Pic/hr. | Current 60-70 Layer thickness 0.5mm |